# writeup for mce-mecn-100k-293k

A translucent colorless block-like specimen of approximate dimensions 0.310 mm x 0.220 mm x 0.090mm, used for the X-ray crystallographic analysis. The chosen specimen was used for both 100K and 293K temperature experiments. The X-ray intensity data were measured on XtaLAB Synergy, Dualflex, HyPix four-circle diffractometer (microfocus sealed x-ray tube, CuKα , λ = 1.54184Å) operated at 50KV voltage and 1mA current. Diffractometer was further equipped with Oxford Cyro system Plus Controller for variable temperature data collection(N2 flow). The frames were integrated with the CrysAlisPro 1.171.43.104a software package. The structure was solved and refined using the SHELXT [1] and SHELXL [2] programs respectively, using the space group type P-1 (no. 2). All non-hydrogen atoms were refined with anisotropic displacement parameters. All hydrogen atoms were found from difference Fourier map. For 100K dataset, hydrogen atom positions and thermal parameters were refined, but for 293K dataset, restrains were applied using SADI and DFIX cards. Following DFIX restraint was applied for hydroxyl hydrogen atom:

DFIX 0.98 O2 H2O

Aromatic hydrogen atoms were restrained to have same distance using the following SADI restraint:

SADI C2 H2 C3 H3 C4 H4 C6 H6 ! AROMATIC C-H DIST

Methyl hydrogens in MCE moiety and solvent MeCN were also restrained using SADI cards.

SADI C8 H8A C8 H8B C8 H8C C9 H9A C9 H9B C9 H9C ! C-H distance
SADI H8A H8B H8A H8C H8B H8C H9A H9B H9A H9C H9B H9C ! H...H non-bonded
SADI C7 H8A C7 H8B C7 H8C ! 1,3-distances

Software used for creating molecular graphics is ORTEP3 [5] for windows/PLATON [3] and packages used for computing publication materials are SHELXLE [4] and WinGX [5] suite of programs.

References:

- Sheldrick, George M. “SHELXT–Integrated space-group and crystal-structure determination.” Acta Crystallographica Section A: Foundations and Advances 71.1 (2015): 3-8.

- Sheldrick, George M. “Crystal structure refinement with SHELXL.” Acta Crystallographica Section C: Structural Chemistry 71.1 (2015): 3-8.

- Spek, Anthony L. “Structure validation in chemical crystallography.” Acta Crystallographica Section D: Biological Crystallography 65.2 (2009): 148-155.

- Hübschle, Christian B., George M. Sheldrick, and Birger Dittrich. ShelXle: a Qt graphical user interface for SHELXL.” Journal of applied crystallography 44.6 (2011): 1281-1284.

- Farrugia, Louis J. “WinGX and ORTEP for Windows: an update” Journal of Applied Crystallography 45.4 (2012): 849-854.