Sonication

In the first set of experiments 3.505 g of metacetamol was dissolved in 100 mL of distilled H2O by overnight stirring on a magnetic stirrer. The next day the solution was filtered and 25 mL of H2O more was added.

For sonication a sonicator with 3 mm probe was used and set to the following parameters: 50 Hz frequency, 0.5 cycle and 40%-100% amplitude (see below). The temperature was kept at ambient conditions, but the ultrasounds caused some local heating; the experiments were done in 14 mL vials, with 5 mL of solution.

Depending on the amplitude the following results and observations were made:

- Amplitude 40% for 15 minutes – after sonication the solution was clear, the vial was left for solvent evaporation, after a week needles started to precipitate -> metacetamol form 1

- Amplitude 60% for 15 minutes – the same as above

- Amplitude 80% for 30 minutes – the same as above; after the sonication the solution was noticeably warm

- Amplitude 100% for 20 minutes – the same as above, after sonication the solution was very hot

We suspect that in the above procedure metacetamol solution was not supersaturated sufficiently, so it’s very important to prepare supersaturated water solution.

The second set of experiments that led to crystallization of hemihydrate entailed preparation of supersaturated water solution of metacetamol at 55°C, cooled down to 33°C and filtrated, which caused partial precipitation (during filtering the solution was further cooled down on its own), but after heating the solution to 35°C, the precipitate dissolved and the solution was clear.

The sonication parameters were set as above, apart from the temperature which was kept at 40°C during the sonication and the amplitude of:

- 40% for 15 minutes – large needles of form 1 (SCXRD)

- 60% for 15 minutes – form 1 (PXRD)

- 80% for 15 minutes – form 1, concomitantly with hemihydrate (PXRD)

- 100% for 15 minutes – after the sonication the solution was clear but soon after large hexagonal crystals appeared at the bottom – these were found to be the crystals of hemihydrate (SCXRD); after a week on the surface of the solution, as well as on the vial walls different smaller crystals appeared, characterized as a hemihydrate (SCXRD).

Mechanochemical grinding

The grinding experiments were performed with a Retsch MM200 ball mill in 10 mL stainless steel jars, using one 10mm stainless steel ball, 25Hz frequency for 60 minutes. Two experiments were performed:

- 145.1 mg of metacetamol and 50 μL of H2O

- 172.4 mg of metacetamol alone

Both experiments did not lead to a phase transition (form 1 was left unchanged; the analysis done by PXRD).

Grinding with 3,4-DHBA (without LAG) produced new crystal phase (cocrystal) stable after weeks of storage. (possible leftovers of MCE-1 are seen in PXRD) – repeat with LAG (MeOH?) for better conversion/crystallinity?

Melting

The experiments were done in 4 mL vials with a cap. The vials with varying amounts of metacetamol (see below) were heated on the heating plate in a heating mantle first to 87°C during 15 minutes, then to 100°C during 8 minutes, then to 150°C during 13 minutes, and finally to 153°C. All samples melted at 151°C, then the heating was turned off – after 78 minutes the temperature in the mantle reached 40°C. Below are the sample weights and results from PXRD analysis:

- 0.1324g -> form 1

- 0.0874g -> form 1

- 0.1160g -> form 1

- 0.3055g -> form 1

To slow down the cooling process which was reported to be the most important parameter, the next set of experiments was done in oil bath in Schlenk vials, filled with argon before the experiments. The heating was done as before and the cooling took 4 hours. This time also form 1 was obtained.

We also tried controlled cooling down after melting the sample at 164°C, with a cooling speed of 6°C/minute. After cooling down to 125°C the sample was solid. Heating and cooling was repeated 4 times. This also resulted in form 1.

The experiments that led to form 2 in a powdered form were conducted in a CHC+ temperature chamber mounted in PXRD diffractometer (detailed description soon).

Crystallization with additives

It was reported for paracetamol that its form 2 could be obtained in a pure form when using pyrazine or pyrazole as additives during crystallization from methanol solution. We tested this approach for metacetamol, but it did not lead (so far) to crystals of form 2. We did obtain a new cocrystal of metacetamol with pyrazine though. Below are the experimental procedures:

- 98 mg of metacetamol and 25 mg of pyrazine dissolved in 200μL of MeOH was kept at the heating plate at 50°C till dissolution, then heated at this temperature for 10 minutes. After taking from the heating plate the sample was sonicated until precipitate occurred –> mecatetamol:pyrazine cocrystal (SCXRD, PXRD)

- 101 mg of metacetamol and 55 mg of pyrazine dissolved in 200μL of MeOH was kept at the heating plate at 50°C till dissolution, then heated at this temperature for 10 minutes. The sample was left for cooling down, after max 1h the crystals started to appear at the bottom –> mecatetamol:pyrazine cocrystal (SCXRD, PXRD)

- 101 mg of metacetamol and 55 mg of pyrazole dissolved in 200μL of MeOH was kept at the heating plate at 50°; because complete dissolution was not achieved, the sample was mildly heated with a gun till dissolution, then left for cooling down. The precipitate appeared quickly at the bottom -> a mixture of metacetamol form 1 and pyrazole (PXRD)

- 98 mg of metacetamol and 44 mg of pyrazole dissolved in 400μL of MeOH was kept at the heating plate at 50° until dissolution, then left to cool down -> a mixture of metacetamol form 1 and pyrazole (PXRD)

- 100 mg of metacetamol and 45 mg of pyrazole dissolved in 450μL of MeOH was kept at the heating plate at 50° until dissolution, then left to cool down -> a mixture of metacetamol form 1 and pyrazole (PXRD)

- 10 mg of metacetamol and 10 mg of 3,4-DHBA dissolved in MeOH -> cocrystal with 3,4-DHBA